Supplementary Data File

Green-Synthesized ZnO–Co₃O₄/C S-Scheme Heterojunction Photocatalyst Derived from Bimetallic ZIF Precursor for Visible-Light-Driven Hydrogen Evolution and CO₂ Reduction

# Table S1. Green metrics comparison between the proposed route and a conventional DMF-based MOF synthesis route.

| Parameter | Conventional DMF-based ZIF synthesis | This work (water–ethanol route) | Improvement / justification |
| --- | --- | --- | --- |
| Solvent type | N,N-dimethylformamide (DMF) | Water–ethanol (1:1 v/v) | Replaces toxic solvent with greener medium |
| CHEM21 classification | Substance of concern | Recommended / lower-risk solvent system | Lower environmental and health risk |
| Boiling point (°C) | 153 | 78 (ethanol), 100 (water) | Lower recovery energy demand |
| E-factor (kg waste/kg product) | ~12.8 | 3.2 | ~75% reduction in waste generation |
| Solvent toxicity | High | Low | Safer handling and disposal |
| Synthesis temperature | 120–150 °C | 120 °C | Comparable thermal demand |
| Synthesis duration | 12–24 h | 12 h | Reduced process time |
| Post-treatment temperature | 600–800 °C | 600 °C | Lower or comparable thermal budget |
| Process scalability | Limited by solvent handling | High | Safer scale-up pathway |

# Table S2. Raw cumulative hydrogen evolution data under visible-light irradiation.

| Time (h) | ZnO Trial 1 | ZnO Trial 2 | ZnO Trial 3 | Co₃O₄/C Trial 1 | Co₃O₄/C Trial 2 | Co₃O₄/C Trial 3 | ZnO–Co₃O₄/C Trial 1 | ZnO–Co₃O₄/C Trial 2 | ZnO–Co₃O₄/C Trial 3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 11.3 | 11.8 | 11.5 | 26.7 | 27.4 | 26.9 | 114.8 | 117.1 | 116.5 |
| 2 | 22.6 | 23.4 | 22.9 | 53.0 | 54.3 | 53.5 | 230.1 | 233.8 | 232.9 |
| 3 | 34.0 | 35.1 | 34.3 | 79.4 | 81.1 | 80.0 | 346.4 | 350.9 | 348.2 |
| 4 | 45.1 | 46.8 | 45.9 | 105.5 | 107.4 | 106.2 | 462.9 | 467.5 | 464.6 |
| 5 | 56.7 | 58.5 | 57.2 | 131.2 | 134.3 | 132.8 | 579.7 | 584.9 | 590.4 |

H₂ evolution rates were calculated using a catalyst mass of 50 mg (0.05 g) and total irradiation time of 5 h.

# Table S3. Derived H₂ evolution rates from triplicate measurements.

| Catalyst | Trial 1 (µmol g⁻¹ h⁻¹) | Trial 2 (µmol g⁻¹ h⁻¹) | Trial 3 (µmol g⁻¹ h⁻¹) | Mean ± SD (µmol g⁻¹ h⁻¹) |
| --- | --- | --- | --- | --- |
| ZnO | 226.8 | 234.0 | 228.8 | 229.9 ± 3.8 |
| Co₃O₄/C | 524.8 | 537.2 | 531.2 | 531.1 ± 6.2 |
| ZnO–Co₃O₄/C | 2318.8 | 2339.6 | 2361.6 | 2340.0 ± 21.4 |

# Table S4. AQY raw data under monochromatic illumination.

| Wavelength (nm) | Incident photons (×10²⁰ photons h⁻¹) | Trial 1 H₂ (µmol h⁻¹) | Trial 2 | Trial 3 | Mean H₂ (µmol h⁻¹) | AQY (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 420 | 2.95 | 5.32 | 5.41 | 5.36 | 5.36 | 7.3 |
| 450 | 2.81 | 5.63 | 5.81 | 5.72 | 5.72 | 8.2 |
| 500 | 2.64 | 4.96 | 5.07 | 5.00 | 5.01 | 7.0 |
| 550 | 2.42 | 3.81 | 3.89 | 3.84 | 3.85 | 5.5 |
| 600 | 2.20 | 2.63 | 2.71 | 2.68 | 2.67 | 3.9 |

Incident photon flux measured using calibrated photodiode and optical power meter; values averaged over three measurements.

# Table S5. Raw product yields for photocatalytic CO₂ reduction over ZnO–Co₃O₄/C.

| Product | Trial 1 (µmol) | Trial 2 (µmol) | Trial 3 (µmol) | Mean ± SD (µmol) | Rate (µmol g⁻¹ h⁻¹) |
| --- | --- | --- | --- | --- | --- |
| CO | 14.4 | 14.8 | 14.85 | 14.68 ± 0.25 | 58.7 ± 1.0 |
| CH₄ | 2.7 | 2.9 | 2.95 | 2.85 ± 0.13 | 11.4 ± 0.5 |
| Total carbon products | 17.1 | 17.7 | 17.8 | 17.53 ± 0.38 | 70.1 ± 1.5 |
| CO selectivity (%) | 84.2 | 83.6 | 83.4 | 83.7 ± 0.4 | — |

# Product formation rates were normalized based on catalyst mass (0.05 g) and reaction duration (5 h).

# Table S6. Control experiments for CO₂ photoreduction.

| Experimental condition | CO detected (µmol) | CH₄ detected (µmol) | Interpretation |
| --- | --- | --- | --- |
| Standard reaction | 14.68 | 2.85 | Normal photocatalytic activity |
| Without catalyst | 0.0 | 0.0 | No catalytic conversion |
| Without light | 0.0 | 0.0 | Light required |
| Under N₂ instead of CO₂ | 0.0 | 0.0 | Carbon products originate from CO₂ |
| Using ¹³CO₂ | 14.5 (¹³CO) | 2.7 (trace ¹³CH₄) | Confirms carbon source from CO₂ |

All control experiments were conducted under identical reaction conditions except for the variable being tested.

# Table S7. BET textural parameters of pristine and heterostructured photocatalysts.

| Sample | BET surface area (m² g⁻¹) | Total pore volume (cm³ g⁻¹) | Average pore diameter (nm) | BET fit R² |
| --- | --- | --- | --- | --- |
| ZnO | 42.3 | 0.118 | 11.2 | 0.9981 |
| Co₃O₄/C | 67.8 | 0.164 | 9.7 | 0.9974 |
| ZnO–Co₃O₄/C (10 wt%) | 112.6 | 0.242 | 8.6 | 0.9986 |
| ZnO–Co₃O₄/C (optimal composition) | 128.3 | 0.287 | 8.1 | 0.9989 |

# Table S8. Raw XRD peak positions and phase assignments.

| Sample | 2θ (°) | d-spacing (Å) | Relative intensity (%) | Miller index (hkl) | Phase assignment |
| --- | --- | --- | --- | --- | --- |
| ZnO | 31.8 | 2.81 | 64 | (100) | ZnO |
| ZnO | 34.4 | 2.60 | 82 | (002) | ZnO |
| ZnO | 36.3 | 2.47 | 100 | (101) | ZnO |
| Co₃O₄/C | 31.3 | 2.85 | 56 | (220) | Co₃O₄ |
| Co₃O₄/C | 36.9 | 2.43 | 100 | (311) | Co₃O₄ |
| Co₃O₄/C | 44.8 | 2.02 | 42 | (400) | Co₃O₄ |
| ZnO–Co₃O₄/C | 31.7 | 2.82 | 51 | (100) | ZnO |
| ZnO–Co₃O₄/C | 36.2 | 2.48 | 78 | (101) | ZnO / overlapping |
| ZnO–Co₃O₄/C | 36.9 | 2.43 | 66 | (311) | Co₃O₄ |

Overlap between ZnO (101) and Co₃O₄ (311) reflections indicating heterojunction formation

# Table S9. Crystallite size estimation from Scherrer analysis.

| Sample | Main peak used | 2θ (°) | FWHM (°) | Calculated crystallite size (nm) |
| --- | --- | --- | --- | --- |
| ZnO | (101) | 36.3 | 0.46 | 18.1 |
| Co₃O₄/C | (311) | 36.9 | 0.68 | 12.3 |
| ZnO–Co₃O₄/C | Composite dominant peak | 36.2 | 0.55 | 15.0 |

# Table S10. Stability cycling raw data.

| Cycle number | H₂ amount after 5 h (µmol) | H₂ retention (%) | CO amount after 5 h (µmol) | CO retention (%) |
| --- | --- | --- | --- | --- |
| 1 | 585.0 | 100.0 | 14.68 | 100.0 |
| 2 | 580.3 | 99.2 | 14.50 | 98.8 |
| 3 | 575.6 | 98.4 | 14.29 | 97.3 |
| 4 | 571.5 | 97.7 | 14.06 | 95.8 |
| 5 | 558.7 | 95.5 | 13.72 | 93.5 |